
**PETROL COKE - Specifications**



**Fuel Grade Raw Petrol Coke**

(Low Sulphur)

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Specification**  **Sl No** | Parameter | | **Unit** | | **Value** |
| **1** | Moisture content (As received) | | % Mass | | 8 max |
| **2** | Ash ( ADB ) | | % Mass | | 1 max |
| **3** | Volatile Matter  ( ADB ) | | % Mass | | 8 min |
| **4** | Fixed Carbon (Calculated) | | % Mass | | 87 min |
| **5** | Total Sulphur  ( ADB ) | | % Mass | | 3.5 to 5 max |
| **6** | | Hargrove Grindability Index (HGI) | | 35-60 min. | |
| **7** | Gross Calorific Value (GCV)( ADB ) | | Kcal/Kg | | 8200 min |